“Linkor-Atlant” LLC

Pavilion 363, #2 Bakchivangi Street, Ekaterinburg, 620910, Russia

Ph: + 7 343 264 06 76. Fax: + 7 343 216 14 66 (65).

Bank Details:

Acct#. 40702840100000020639

Public Corporation “SKB-bank”, Ekaterinburg

(swift SKBERU4E)

Correspondence bank:  Raiffeisen Zentralbank Oesterreich,

Vienna, Austria (swift RZBAATWW), Acct# 70-55.068.654

| http://www.lin-kor.ru E-mail: lin-kor@yandex.ru Phone: +7(343) 214-81-31, 216-14-66, 226-67-56 Fax: +7(343) 264-06-76 |  |  |
| --- | --- | --- |

STRUCTURE AND COMPOSITION

of decorative quartz-vinyl tile

GRANDECO TILE

TILE (SQUARE, WOOD, CLASSICS)

| MAIN COMPONENTS | CONTENT |
| --- | --- |
| PITCH of polyvinylchloride | 40.80% |
| PLASTICIZER (D.O.P.) | 8.26% |
| STABILIZER OF HIGH TEMPERATURE | 3.10% |
| LUBRICANT | 0.04% |
| COMPLEX STABILIZER | 0.80% |
| FILL MATERIAL | 47.00% |
| TOTAL | 100% |

Composition of substances for each layer

<3.0mm, 0.5mm Wood, Classics & Montana>

| Layer | Width | PVC | DOP | Stabilizer | Filler (%) |
| --- | --- | --- | --- | --- | --- |
| UV Covering | 0.02mm | - | - | - | - |
| Protective layer | 0.50mm | 70~80 | 15~25 | 0~6 | - |
| Printed layer | 0.07mm | 70~80 | 15~25 | 0~6 | - |
| Central layer | 1.63mm | 50~70 | 5~8 | few | 25~45 |
| Base | 0.78mm | 50~80 | 8~15 | 0~6 | 10~30 |
| * Protective layer & Printed layer : natural PVC * Central layer & Base : Worked over PVC * Filler : CaCO3 |